## Slide 1
Cobalt free, Single Crystal LMNO Spinel (Model HPS55)
Next generation cathode active material; LiMn1.5-xNi0.5-yMx+yO4
Superior safety
2. High specific energy with flat potential at 4.7V vs Li/Li+
3. Cobalt free and less Nickel (Manganese rich)
High rate capability
Compatible with aqueous binder

## Slide 2
Top Battery LMNO(HPS55) is single crystal structure and shows superior safety
compared with other commercial cathode material.
It decomposes at much higher temperature without significant heat flow.
Differential scanning calorimeter(DSC) analysis
with various cathode material
Sample | Onset temperature (℃) | Peak temperature (℃) | Enthalpy (J g-1)
NCM811 | 197.8 | 208.7 | 1514
LCO | 257.2 | 261.4 | 1665
LFP | 251.1 | 275.5 | 99
LMO | 263.4 | 270.9 | 1450
LMNO | 302.4 | 338.1 | 931
Chart: Temperature (℃)
Scan rate : 5℃/min
<Test method>
Electrode is made with each cathode material;
Coin cell is assembled with Li counter electrode;
Each coin cell is disassembled in fully charged state;
Electrode is rinsed with dimethyl carbonate;
Each powder is collected and analyzed by DSC

## Slide 3
Chart: Capacity (mAh/g)
High specific capacity at high flat potential
2032 coin cell with Li counter electrode
Charge : CCCV, 0.1C, 4.9V, 0.05C cut off
Discharge : CC, 0.1C, 3.0V Cut off
The specific capacity of HPS55 is over 135mAh/g with high flat potential at 4.7V.
The specific energy is compatible with NCM622.
Cathode Material | Specific capacity (mAh/g) | Discharge potential (Volt) | Specific energy (Wh/kg)
NCM622 | 170 | 3.65 | 621
NCM811 | 190 | 3.65 | 694
LFP | 135 | 3.25 | 439
LMO | 105 | 3.85 | 404
LMNO(HPS5) | 137 | 4.70 | 644

## Slide 4
Chart: Capacity (mAh/g)
High C rate capability
2032 coin cell with loading of 0.9mAh/cm2
Charge : CCCV, 1C, 4.9V, 0.05C cut off
Discharge : CC, 0.5C, 1C, 3C, 5C, 10C, 3.0V Cut off
Single crystal HPS55 is optimal structure for Li+ diffusion.
Cathode composition of 2wt% conductive carbon and 2wt% PVdF binder
shows superior high rate discharge capability.

## Slide 5
Good cycle life at room and high temperature
Single crystal HPS55 shows good cycle life with Li counter electrode.
Chart: Cycle Number
2032 coin cell with loading of 0.9mAh/cm2
Charge : CCCV, 1C, 4.9V, 0.05C cut off
Discharge : CC 1C, 3.0V Cut off

## Slide 6
Good cycle life at 21700 cylindrical cell of LMNO/LTO
Single crystal HPS55 shows good cycle life with Li4T5O12 anode.
Chart: Cycle No.
21700 cylindrical cell with loading of 3.0mAh/cm2
Charge : CCCV, 0.3C, 3.4V, 0.05C cut off
Discharge : CC 0.5C, 2.5V Cut off

## Slide 7
Specification and Certificate of analysis
ITEM |  | Unit | Specification | Result | Remark
Particle Size | D10 | μm | ≥1.0 | 2.481 | Laser particle size analyzer
 | D50 |  | 4.0 – 7.0 | 5.832 | 
 | D90 |  | <20.0 | 15.63 | 
Tap Density |  | g/cm3 | ≥1.60 | 1.62 | ISO 3953 (250tap/min, 5min)
Specific capacity @0.1C |  | mAh/g | ≥ 130mAh/g | 137.6mAh/g | 2032 Coin Cell (3.0V – 4.9V, Li CE) 0.9mAh/cm2
1st Cycle efficiency |  | % | ≥ 88% | 88.5% |